Tetra-Function Novolac Type

| TRADE NAME | EPOXY EQUIVALENCY (g/eq) | NON VOLATILITY (wt%) | COLOR (Gardner) | CHARACTERSTICS |
| --- | --- | --- | --- | --- |
| GEPN431A70 | 200-240 | 69-71 | 9-13 | Tetrafunction resin,excellent for heat-resistance and UV-blocking |